| DIAMCALC ILLUSTRATED REPORT |  |  | Parameter | Avg | Min | Max | Dev | Cut | Sym |  |  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Polished Brilliant |  |  |  | Diameter, mm | 6.014 | 5.999 | 6.038 | 0.65% | N/A | EX |  |  | 6.027 | 6.017 | 6.005 | 6.004 |  |  |  |  |
|  |  |  |  | Crown angle, ° | 33.58 | 33.35 | 33.70 | 0.35 | N/A | EX |  |  | 33.64 | 33.70 | 33.55 | 33.67 | 33.35 | 33.53 | 33.67 | 33.55 |
|  |  |  |  | Pavilion angle, ° | 40.89 | 40.57 | 41.14 | 0.58 | N/A | EX |  |  | 40.57 | 40.67 | 40.84 | 41.08 | 41.14 | 41.08 | 41.00 | 40.70 |
| Model | Sample Sarin Model |  |  | Total height, % | 62.66 |  |  |  | N/A | - |  |  |  |  |  |  |  |  |  |  |
| Expert name | Sample Expert Name |  |  | Crown height, % | 14.33 | 14.00 | 14.58 | 0.58 | N/A | EX |  |  | 14.36 | 14.58 | 14.32 | 14.32 | 14.38 | 14.32 | 14.34 | 14.00 |
| Report date | 12/09/2006 |  |  | Pavilion depth, % | 43.00 | 42.69 | 43.28 | 0.59 | N/A | EX |  |  | 42.93 | 42.99 | 43.06 | 43.28 | 43.08 | 42.99 | 43.01 | 42.69 |
| Real weight, ct | 0.86 |  |  | Table, % | 56.61 | 56.25 | 56.85 | 0.59 | N/A | EX |  |  | 56.55 | 56.25 | 56.78 | 56.85 |  |  |  |  |
| Calculated weight, ct | 0.86, 0.8662 |  |  | Culet, % | 0.68 | 0.54 | 0.80 | 0.26 | 0 | EX |  |  |  |  |  |  |  |  |  |  |
| Measurements, mm | 6.014 (5.999-6.038) x 3.769 /0.007 |  |  | Girdle Bezel, % | 5.30 | 4.91 | 5.93 | 1.02 | 3 | EX |  |  | 5.36 | 5.10 | 5.31 | 4.91 | 5.21 | 5.33 | 5.26 | 5.93 |
| Spread | -0.05 ct, -6.74% |  |  | Girdle Bone, % | 5.34 | 4.76 | 5.63 | 0.87 | - | EX |  |  | 5.18 | 5.24 | 4.76 | 5.52 | 5.63 | 5.48 | 5.39 | 5.52 |
|  |  |  |  | Girdle Valley, % | 3.74 | 3.24 | 4.09 | 0.85 | 0 | EX |  |  | 3.73 | 3.41 | 3.50 | 3.59 | 3.53 | 3.24 | 3.71 | 3.85 |
| Average values, mm |  |  |  |  |  |  |  |  |  |  |  | 3.74 | 3.87 | 3.97 | 3.97 | 3.75 | 3.80 | 4.05 | 4.09 |
|  |  |  | Star: | 54.18: | 51.53: | 55.60: | 4.07 | - | - |  |  | 55.60: | 55.21: | 53.61: | 54.59: | 51.53: | 53.08: | 54.98: | 54.82: |
| Total height | Crown height | Pavilion depth | Table | Culet | Girdle |  |  | Upper ratio, % | 45.82 | 48.47 | 44.40 |  |  |  |  |  | 44.40 | 44.79 | 46.39 | 45.41 | 48.47 | 46.92 | 45.02 | 45.18 |
|  |  |  |  |  | Bezel | Bone | Valley |  |  | Star angle, ° | 21.56 | 20.82 | 22.41 | 1.59 |  | VG |  |  | 21.92 | 21.66 | 22.41 | 21.48 | 20.82 | 21.09 | 21.53 | 21.54 |
| 3.769 | 0.862 | 2.586 | 3.405 | 0.041 | 0.319 | 0.321 | 0.225 |  |  | Upper girdle angle, ° | 40.58 | 39.55 | 41.63 | 2.08 | - | GD |  |  | 41.11 | 41.10 | 41.19 | 41.06 | 40.35 | 40.66 | 40.04 | 40.19 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 39.55 | 39.70 | 39.83 | 40.28 | 40.26 | 41.01 | 41.27 | 41.63 |
|  |  |  | Lower girdle angle / Halves angle, ° | 41.86 | 41.54 | 42.19 | 0.65 | - | EX |  |  | 41.57 | 41.59 | 41.68 | 41.83 | 41.88 | 41.97 | 42.19 | 42.11 |
|  |  |  |  |  |  |  |  |  |  |  |  | 42.11 | 42.16 | 42.04 | 42.03 | 41.80 | 41.69 | 41.61 | 41.54 |
|  |  |  | Twist, ° | 0.74 | 0.01 | 1.66 | 1.65 | - | EX |  |  | 0.17 | 0.01 | 0.31 | 0.65 | 0.55 | 1.66 | 1.53 | 1.09 |
|  |  |  | Crown height, mm | 0.862 | 0.842 | 0.877 | 0.035 | - | - |  |  | 0.864 | 0.877 | 0.861 | 0.861 | 0.865 | 0.861 | 0.862 | 0.842 |
|  |  |  | Pavilion depth, mm | 2.586 | 2.568 | 2.603 | 0.035 | - | - |  |  | 2.582 | 2.585 | 2.590 | 2.603 | 2.591 | 2.586 | 2.587 | 2.568 |
|  |  |  | Table, mm | 3.405 | 3.383 | 3.419 | 0.036 | - | - |  |  | 3.401 | 3.383 | 3.415 | 3.419 |  |  |  |  |
|  |  |  | Culet, mm | 0.041 | 0.033 | 0.048 | 0.016 | - | - |  |  |  |  |  |  |  |  |  |  |
|  |  |  | Girdle Bezel, mm | 0.319 | 0.295 | 0.357 | 0.061 | - | - |  |  | 0.323 | 0.307 | 0.320 | 0.295 | 0.313 | 0.320 | 0.316 | 0.357 |
|  |  |  | Girdle Bone, mm | 0.321 | 0.286 | 0.339 | 0.053 | - | - |  |  | 0.312 | 0.315 | 0.286 | 0.332 | 0.339 | 0.330 | 0.324 | 0.332 |
|  |  |  | Girdle Valley, mm | 0.225 | 0.195 | 0.246 | 0.051 | - | - |  |  | 0.224 | 0.205 | 0.211 | 0.216 | 0.212 | 0.195 | 0.223 | 0.232 |
|  |  |  |  |  |  |  |  |  |  |  |  | 0.225 | 0.233 | 0.239 | 0.239 | 0.226 | 0.229 | 0.243 | 0.246 |
|  |  |  | Measurement as per OctoNus theory: |  |  |  |
|  |  |  | Crown angle, ° | 33.58 | 33.50 | 33.62 | 0.12 | - | - |  |  | 33.50 | 33.62 | 33.61 | 33.61 |  |  |  |  |
|  |  |  | Pavilion angle, ° | 40.89 | 40.86 | 40.92 | 0.06 | - | - |  |  | 40.86 | 40.87 | 40.92 | 40.89 |  |  |  |  |
|  |  |  | Fish eye effect, ° | 8.65 | N/A | - |  |  | Extra Facet / Nat | No |
|  |  |  | Culet through Crown Bezel, ° | 10.59 | N/A | - |  |  | Girdle to MIC, mm | 0.007 |
|  |  |  | Parameter, ° | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |  |  |  |
|  |  |  | Pav. azimuths deviation from ideal | 0.00 | -0.47 | -0.06 | -0.30 | -1.28 | 0.01 | 0.34 | -1.73 |  |  |  |
|  |  |  | Crown azimuths deviation from ideal | -0.17 | -0.47 | -0.37 | -0.95 | -0.74 | -1.65 | -1.18 | -0.64 |  |  |  |
|  |  |  | Crown painting | -0.32 | -0.14 | 0.39 | 0.29 | -0.42 | -0.66 | -0.52 | -0.85 |  |  |  |
|  |  |  |  | -0.87 | -1.34 | -0.17 | -0.61 | -0.92 | -0.20 | 0.35 | 1.89 |  |  |  |
|  |  |  | Pavilion painting | -0.81 | 0.14 | -0.02 | 0.12 | -0.19 | -0.06 | -0.64 | -0.16 |  |  |  |
|  |  |  |  | 0.12 | 0.55 | -0.18 | 0.49 | -1.63 | -0.10 | 0.34 | 1.46 |  |  |  |
| Appraiser title | AGS_2005 |  |  |  |  |  |  |  |
| Overall cut quality | 3 |  |  |  |  |  |  |  |
| Overall symmetry quality | PR |  |  |  |  |  |  |  |
| Symmetry |  |  |  |  |  |  |  |  |
| Polish |  |  |  |  |  |  |  |  |
| Color |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  | Girdle center |  | Culet center |  | Тable center |  |  | Paint / Dug | Avg | Max | Type |
| Clarity |  |  |  | Offset by table axis |  |  | Crown, ° | -0.26 | 1.89 |  |
|  |  |  |  | Girdle-Culet | 0.37 ± 0.20, % | 0.023 ± 0.012, mm |  |  | Crown, notches | 0.1, Absent | 0.5 |  |
| Fluorescence |  |  |  | Girdle-Table | 0.12 ± 0.18, % | 0.007 ± 0.011, mm |  |  | Pavilion, ° | -0.03 | -1.63 |  |
|  |  |  |  | Table-Culet | 0.44 ± 0.22, % | 0.026 ± 0.013, mm |  |  | Pavilion, notches | 0.0, Absent | 0.4 |  |