| HELIUM ILLUSTRATED REPORT |  | Brilliant 0.2309 ct |  | Brilliant 0.2420 ct |
| --- | --- | --- | --- | --- |
| Rough diamond | July 21, 2010 |  | Clarity: VVS2, Color: H, Grade: 0 |  | Clarity: VVS2, Color: H, Grade: 0 |
|  |  |  | Rough weight | 0.4524, ct | Yield | 51.11, % |  | Rough weight | 0.5362, ct | Yield | 45.28, % |
|  |  |  | Tilting | 66.71, ° | Next part | 0.5924, ct |  | Tilting | 112.92, ° | Next part | 0.5777, ct |
| Rough weight, ct | 1.0448 (0.5362 + 0.4524) |  | Distance to Holder | 3.755, mm | Price | 414.00, $ |  | Distance to Holder | 3.756, mm | Price | 432.00, $ |
| Diamonds weight, ct | 0.4729 (0.2309 + 0.2420) |  |  |  |  |
| Yield, % | 45.19 (45.28, 51.11) |  | Parameters |  |  | Grade |  | Parameters |  |  | Grade |
| Saw plane width, mm | 0.180 |  | Diameter min, max | 3.962, mm | 3.942, mm | 0 |  | Diameter min, max | 4.034, mm | 4.054, mm | 0 |
| Saw quantity | 1 |  | Girdle ratio | 0.995 |  |  |  | Girdle ratio | 1.005 |  |  |
| Saw weight | 0.0562, ct; 5.38 % |  | Pavilion angle | 40.75, ° |  | N/A |  | Pavilion angle | 41.20, ° |  | N/A |
| Appraiser | AGS_Classic |  |  |  |  |  |  |  |  |  |  |
| Price list | Rapaport: 09 july 2004 |  | Crown angle | 35.00, ° |  | 0 |  | Crown angle | 35.10, ° |  | 0 |
| Diamonds price, $ | 846.00 (414.00 + 432.00) |  | Total depth | 61.17, % | 2.423, mm | N/A |  | Total depth | 61.18, % | 2.468, mm | N/A |
|  |  | Pav depth bezel | 43.08, % | 1.707, mm | 0 |  | Pav depth bezel | 43.77, % | 1.766, mm | 0 |
|  |  | Crown height bezel | 14.88, % | 0.589, mm | N/A |  | Crown height bezel | 14.93, % | 0.602, mm | N/A |
|  |  | Girdle bezel | 3.20, % | 0.127, mm | N/A |  | Girdle bezel | 2.47, % | 0.100, mm | N/A |
|  |  | Pav depth valley | 43.94, % | 1.741, mm | N/A |  | Pav depth valley | 44.64, % | 1.801, mm | N/A |
|  |  | Crown height valley | 15.72, % | 0.623, mm | N/A |  | Crown height valley | 15.78, % | 0.637, mm | N/A |
|  |  | Girdle valley | 1.50, % | 0.059, mm | 0 |  | Girdle valley | 0.75, % | 0.030, mm | 0 |
|  |  | Table | 57.50, % | 2.278, mm | 0 |  | Table | 57.50, % | 2.319, mm | 0 |
|  |  | Culet | N/A, % | N/A, mm | N/A |  | Culet | N/A, % | N/A, mm | N/A |
|  |  | Lower facets | 82.00, % |  | N/A |  | Lower facets | 82.00, % |  | N/A |
|  |  | Culet through bezel | 10.58, ° |  | 0 |  | Culet through bezel | 10.41, ° |  | 0 |
|  |  | Fish eye effect | 49.88, ° |  | 0 |  | Fish eye effect | 48.10, ° |  | 0 |
| Notes: |  |  |  |  |  |  |  |  |  |  |  |