| ILLUSTRATED REPORT FOR ANY CUT |  |  | Parameter | Avg | Min | Max | Dev |  |  | Facets' slope angles |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Pear | 02.07.2008 |  |  | Diameter, mm |  | 5.802 | 6.792 | 17.07 % |  |  |  |  |
|  |  |  |  | Crown height, % | 14.09 | 13.23 | 15.16 | 1.93 |  |  |  |  |
| Model | Simple |  |  | Crown height, mm | 0.957 | 0.899 | 1.030 | 0.131 |  |  |  |  |
| Expert name | Makoed A.G. |  |  | Pavilion depth, % | 45.95 | 44.91 | 48.34 | 3.43 |  |  |  |  |
| Real weight, ct | 1.00 |  |  | Pavilion depth, mm | 3.121 | 3.050 | 3.283 | 0.233 |  |  |  |  |
| Calculated weight, ct | 1.02, 1.0203 |  |  | Girdle Bezel, % | 4.08 | 2.33 | 5.76 | 3.44 |  |  |  |  |
| Spread | -0.19 ct, -22.81 % |  |  | Girdle Bezel, mm | 0.277 | 0.158 | 0.392 | 0.234 |  |  |  |  |
| Extra Facet / Nat | No |  |  | Girdle Valley, % | 2.91 | 1.91 | 3.58 | 1.67 |  |  |  |  |
|  |  |  |  | Girdle Valley, mm | 0.198 | 0.129 | 0.243 | 0.114 |  |  |  |  |
| Width | Length | Ratio (L/W) | Diameter Minimum | Diameter Maximum | Girdle Ratio |  |  | Table, % |  | 52.59 | 56.24 | 3.65 |  |  |  |  |
|  |  |  |  |  |  |  |  | Table, mm |  | 3.051 | 3.820 | 0.769 |  |  |  |  |
| 6.792 mm | 5.802 mm | 0.854 | 5.802 mm | 6.792 mm | 1.171 |  |  | Culet, % |  | 0.43 | 0.56 | 0.12 |  |  |  |  |
|  |  |  |  |  |  |  |  | Culet, mm |  | 0.030 | 0.038 | 0.008 |  |  |  |  |
| Total height | Crown height | Pav. depth | Girdle |  |  |  |  |  |  |  | Facets' azimuth angles |
|  |  |  | Bezel | Valley |  |  |  |  |  |  |  |  |  |
| 4.437 mm 65.32 % | 0.957 mm | 3.121 mm | 0.277 mm | 0.198 mm |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  | Facets’ heights (%) |
|  |  |  | Girdle asymmetry | Recommendation for girdle asymmetry removing |  |  |  |  |
|  |  |  |  |  |  |  |  |  | Girdle facets’ angles & MIC | Girdle facets’ azimuth & MIC |
| Appraiser title | GIA_PCTG_StarCul |  |  |  |  |  |  |  |  |  |  |
| Overall cut quality | N/A |  |  |  |  |  |  |  |  |  |  |
| Symmetry appraiser title | Internal |  |  |  |  |  |  |  |  |  |  |
| Overall symmetry quality | PR |  |  |  |  |  |  |  |  |  |  |
| Color |  |  |  |  |  |  |  |  |  |  |  |
| Clarity |  |  |  |  |  |  |  |  |  |  |  |
| Polish |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  | Girdle-Culet offset by table axis | 9.12 ± 0.23, % | 0.619 ± 0.015, mm |  |  |  |  |
| Fluorescence |  |  |  | Girdle-Table offset by table axis | 6.61 ± 0.20, % | 0.449 ± 0.013, mm |  |  |  |  |
|  |  |  |  | Table-Culet offset by table axis | 2.56 ± 0.24, % | 0.174 ± 0.016, mm |  |  |  | Girdle center |  | Culet center |  | Тable center |  | MIC center |