| HELIUM FULL REPORT | Semi-polished Rounded Fancy |
| --- | --- |
| General information |  |
| Model | Simple |  |
| Expert name | Makoed A.G. |  |
| Report date | 05.07.2007 |  |
| Real weight, ct |  |  |
| Calculated weight, ct | 1.18, 1.1869 |  |
| Spread | 0.27 ct, 18.90% |  |

## Main parameters

| Parameter |  | Avg | Min | Max | Dev |
| --- | --- | --- | --- | --- | --- |
| Diameter | mm | 8.141 | 5.428 | 11.077 | 104.06 %, 5.649 mm |
| Pavilion depth | % | 42.84 | 42.51 | 43.10 | 0.58 |
| Pavilion depth | mm | 2.326 | 2.308 | 2.339 | 0.032 |
| Pavilion depth at girdle minima | % | N/A | N/A | N/A | N/A |
| Pavilion depth at girdle minima | mm | N/A | N/A | N/A | N/A |
| Crown height | % | 12.95 | 11.31 | 13.88 | 2.58 |
| Crown height | mm | 0.703 | 0.614 | 0.754 | 0.140 |
| Crown height at girdle minima | % | 11.17 | 11.17 | 11.17 | 0.00 |
| Crown height at girdle minima | mm | 0.606 | 0.606 | 0.606 | 0.000 |
| Total height | % | 60.53 |  |  |  |
| Total height | mm | 3.286 |  |  |  |
| Table | % | 67.35 | 60.69 | 74.02 | 13.32 |
| Table | mm | 5.747 | 3.295 | 8.199 | 4.904 |
| Culet | % | 0.93 | 0.45 | 1.35 | 0.91 |
| Culet | mm | 0.051 | 0.024 | 0.073 | 0.049 |
| Girdle thickness: Bezel | % | 5.30 | 3.55 | 12.50 | 8.94 |
| Girdle thickness: Bezel | mm | 0.288 | 0.193 | 0.678 | 0.486 |
| Girdle thickness: Valley | % | 11.81 | 11.81 | 11.81 | 0.00 |
| Girdle thickness: Valley | mm | 0.641 | 0.641 | 0.641 | 0.000 |

| Offset |  | Distance | Width wise | Length wise |
| --- | --- | --- | --- | --- |
| Culet-Table offset by table axis | % | 1.32 ± 0.35 | 0.07 | 1.32 |
| Culet-Table offset by table axis | mm | 0.072 ± 0.019 | 0.004 | 0.071 |
| Girdle-Culet offset by table axis | % | 1.21 ± 0.34 | 0.14 | 1.20 |
| Girdle-Culet offset by table axis | mm | 0.066 ± 0.018 | 0.007 | 0.065 |
| Girdle-Table offset by table axis | % | 0.23 ± 0.31 | 0.20 | 0.11 |
| Girdle-Table offset by table axis | mm | 0.013 ± 0.017 | 0.011 | 0.006 |
| Girdle to table-culet line offset | % | 0.31 |  |  |
| Girdle to table-culet line offset | mm | 0.017 |  |  |

| Culet shift ratio by width & length |  |
| --- | --- |
| Width | 5.428 mm, 100% |
| Width-wise culet shift ratio | 2.723 mm, 50.17 % | 2.708 mm, 49.88 % |
| Length | 11.077 mm, 100% |
| Lengh-wise culet shift ratio | 5.473 mm, 49.41 % | 5.604 mm, 50.59 % |

| Culet shift ratio by main diameter |  |
| --- | --- |
| Main diameter (width) | 5.428 mm, (100%) |
| Width-wise culet shift ratio | 2.723 mm, 50.17 % | 2.708 mm, 49.88 % |
| Lengh-wise culet shift ratio | 5.473 mm, 100.83 % | 5.604 mm, 103.24 % |

## Pavilion and crown views of the diamond with indication of the diameter minimum and maximum

Invisible edges are hidden

Invisible edges are drawn taking refraction into account

## Plots

Girdle thickness plot

Diameter variation plot

## Facets' azimuth and slope angles

Pavilion and crown views of the diamond with indication of facets' azimuth angles

Pavilion and crown views of the diamond with indication of facets' slope angles

## Facets' heights

Pavilion and crown views of the diamond with indication of facets' heights (mm)

Pavilion and crown views of the diamond with indication of facets' heights (%)

## Additional illustrations

Pavilion and crown views of the diamond with indication of invisible edges without refraction

|  | Girdle center |  | Culet center |  | Table center |
| --- | --- | --- | --- | --- | --- |